Monte-Carlo-Simulation Study of the selforganization of nanometric amorphous precipitates in regular arrays during ion irradiation

F. Zirkelbach, M. Häberlen, J.K.N. Lindner, B. Stritzker

Universität Augsburg, Universitätsstrasse 1, D-86135 Augsburg, Germany.

# Abstract

High-dose ion implantation of materials that undergo a drastic density change upon amoprhization result in periodically arranged, selforganized, nanometric structures of the amorphous phase at certain implantation conditions. A simple model explaining the phenomenon is introduced and applied to a Monte-Carlo-Simulation code in order to better understand the process of selforganization. Conditions for observing such lamellar precipitates can be specified and additional information about the compositional and structural state during the ordering process is gained by simulation.

PACS codes:

Keywords: 	Monte-Carlo Simulation, selforganization, precipitation, amorphization, nanostructures, ion irradiation

# Introduction

Owing to the statistical nature of collision processes, ion implantation into solids in a first place leads to disordered systems, such as depth profiles of different defects or distributions of precipitates with variable size. Ion implantation could be an elegant technique to create nanostructured surface regions, however, the statistics involed puts limits to those applications where existing fluctuations can be tolerated. These limits may be overcome by driving the system strongly by ion irradiation and simultaneously having mechanisms which counteract the irradiation effect. Under these circumstances selforganization can take place and allow for much more ordered systems to develope. Surface ripple formation during ion erosion is a prominent example for such an effect (sputtering is counteracted by surface diffusion), and implantation induced precipitate formation accompanied by ballistic precipitate destruction leading to narrow precipitate size distributions is another.

In the present paper we explore a selforganization process which leads to regular arrays of amorphous spherical or lamellar nano-inclusions and which has been observed for a number of ion/target combinations, e.g. O+ or C+ implantation into Si, Ar+ into Al2O3 or Si+ into SiC. All these systems have in common that the amorphous phase has a largely reduced density of host atoms compared to the crystalline host lattice. Therefore the amorphous inclusions exert compressive stress on the host matrix, leading to their selforganized spacial arrangement. In the present work we focus on high-dose carbon implantations into silicon.

# Mechanisms contributing to amorphization

If high-dose carbon implantations are performed at sufficiently high implantation temperatures to prevent complete surface amorphization and at the same time sufficiently low temperatures to prevent direct formation of crystalline 3C-SiC precipitates, it has been shown [1] that the carbon supersaturation of the crystalline silicon (c-Si) matrix is reduced by the formation of carbon rich amorphous precipitates (a-SiCx) with few nanometers in size. An example of amorphous nano-inclusions is presented in the cross-sectional transmission electron microscopy bright field images in Figure 1, showing amorphous lamellae and spheres in Si(100) implanted at 150°C with 4.3 x 1017 cm-2 180 keV C+ ions. The precipitation of carbon in an amorphous a-SiCx phase helps the system to save the enormous interfacial energy which would be required if an interface was built up between crystalline 3C-SiC and c-Si with 20 % lattice mismatch. Pure amorphous silicon (a-Si) would not be stable against ion beam induced epitaxial recrystallization under the present implantation conditions, but small amounts of carbon are known to stabilize the a-Si phase [2]. Vice versa, the fact that the light C+ ions can amorphize c-Si at all at these elevated temperatures is attributed to the presence of carbon impurities, the effect termed “carbon induced amorphization” [3].  Once small a-SiCx inclusions have been formed they may serve as diffusional sinks for excess carbon atoms in the c-Si phase (the room temperature solid solubility of C in c-Si beeing essentially zero). By this the a-SiCx phase can grow. Since the Si atomic density of stoichiometric amorphous SiC is 20-30% smaller than that of c-Si [4,5], a reduced density is assumed also for relaxed substoichiometric a-SiCx. In the unrelaxed state the a-SiCx inclusions are assumed to exert compressive stress on their surrounding which decays by a r-2 law. This stress is partially compensated by arranging the a-SiCx spheres in regular arrays. Such local stress fields have been shown [6] to enhance the local probability for further amorphization, as perfect crystall lattice restoration after an ion impact is less likely than in unstrained c-Si, leading to the formation of amorphous lamellae by connecting the amorphous spheres laterally. These lamellae develope preferentially parallel to the surface as strain relaxation perpendicular to the surface can be easily achieved. As a sum, there are mainly three mechanisms leading to amorphization, normal “ballistic” amorphization, carbon induced amorphization, and stress enhanced amorphization. It is assumed that ion beam induced amorphous to crystalline transitions can also occur, however,they are unlikely if the entire surrounding is already amorphized since then the necessary structural information is absent.

# Monte-Carlo Simulation

As the simulation focuses on the selforganiztion process of lamellar precipitates which takes place below the continuous a-SiCx layer some usefull approximations simplify the algorithm. In case of 180 keV C+ in Si the interested depth region, furtheron called simulation window, is between 0 and 300 nm. The nuclear stopping power and the implantation profile gained by TRIM [7] simulation results may be approximated by a linear function of depth in the mentioned depth region without having too big variations from the real profile.

For the algorithm this section of the target is devided into 64x64x100 volumes with a side length of 3 nm. Each volume keeps information about its amorphous or crystalline state and the incorporated amount of carbon. For further considerations the volumes need to be addressable which is done by the position vector r=k,l,m with k,l∈0,64 and m∈0,100.

A simulation loop corresponds to an iplanted carbon ion which moves through the target effecting collisions with silicon atoms turning volumes in the amorphous or crystalline state, incorporation somewhere in the target and finally a possible diffusion of carbon from crystalline to neighboured amorphous volumes. Therefor the algorithm is devided in three parts, the amorphizaion/recrystallization process, the carbon incorporation and the carbon diffusion.

As amorphization occurs more likely at high energy transfers the volumes that get hit by a carbon ion are determined by two random numbers x,y∈0,1 using a uniform probability distribution, p(x)dx=dx, p(y)dy=dy, mapped to the coordinates k,l and a random number z distributed according to the linear approximated nuclear stopping power, p(z)=(sz+s0)dz, with s and s0 identifying the nuclear energy loss, mapped to the m coordinate. After that an amorphization probability composed of three parts taking into account ballistic, carbon-induced and stress-induced amorphization is calculated. The ballistic amorphization probability pb being proportional to the nuclear energy loss is a constant in the simulation as the collision localization already takes care of the nuclear energy loss. The carbon-induced probability is proportional to the local carbon concentration. The stress-induced part results from compressive stress of the amorphous carbon-rich neighbours, the stress amplitude increasing with respective carbon concentration, decreasing with the square of the distance d=r−r'. Thus the amorphization probability pc→a of a crystalline volume is

pc→a(r)=pb+pcccarbon(r)+psamorphousneighboursccarbon(r')d.

pb, pc and ps are simulation parameters weighting the three different ways of amorphization. The recrystallization probability pa→c of an amorphous volume is assumed as

pa→c=1−pc→a.

Another random number finally determines whether the volume turns amorphous, recrystallizes or remains unchanged. The number of average hits per implanted ion is extracted from TRIM [7] collsion data.

In the second part random coordinates for the ion incorporation are determined. Again k,l are obtained by a uniform probability ditribution while m emanates from a probability distribution according to the linear approximated implantation profile.

In order to allow reduction of supersaturation of carbon in crystalline volumes carbon diffusion is regarded as a last step of the simulation every dv itterations, moving dr of the amounnt of carbon in crystalline cells to an amorphous neighbour. Beside dv and dr being simulation parameters describing the diffusion rate, a switch to exclude diffusion in z-direction is implemented. As diffusional broadening of carbon concentration profiles have not been observed even at much higher target temperatures where no amorphous phase is formed [8], diffusion among crystalline volumes are not regarded.

Steps s and dose d are connected by

d=s(64∗64)(3nm)2,

e.g. 30,000,000 steps are equivalent to a dose of 0.81 1017cm-2.

# Results

In Figure 2 several simulation results with different simulation parameters are compared. Black volumes represent crystalline SiCx while amorphous volumes are white. The results allow to specify conditions for observing lamellar structures.

The assumption of stress mediated amorphization as a mechanism contributing to lamellae formation is confirmed in Figures 2 (a,b,c,d) that show the results of four identical simulation runs with increasing stress influence ps leading to systematically enlarged extensions of the lamellae zone and additionaly increasing mean diameter of the amorphous precipitates.

The impact of the diffusion process is shown in Figures 2 (e,f) and 2 (g,h). Higher diffusion rates (Figure 2 (f)) result in larger depth domains of lamellar structure as due to the mobile carbon amorphous volumes, even at lower depth regions, hold more carbon which stabilizes the amorphous state. In contrast for, less mobile carbon (Figure 2 (e)) the redistribution of carbon is too slow arranging for carbon-rich amorphous volumes not being affected by recrystallization. The importance of diffusin gets evident in Figures 2 (g,h) showing the results of two identical simulation runs with diffusion in z-direction switched off (Figure 2(g)) and on (Figure 2 (h)). Lamellar structures are only observed in the case of enabled diffusion. Amorphous volumes enhance stability against recrystallization by depriving crystalline volumes in surrounding layers of carbon. While the probability of amorphization in that layer is increased due to the enlarged stress term resulting from the carbon-rich amorphous precipitate the amorphization in the carbon denuded volumes and their latteral vicinity is decreased. This obviously fortifies the selforganization process.

As a consequence the amorphous and crystalline lamellae have a complementary arrangement in neighbouring layers m and m+1 as shown in Figure 3 (a,b). The carbon map (Figure 3 (c,d)) verifies the carbon accumulation in the amorphous precipitates and the carbon denuded crystalline area.

The compressive stress is visualized in Figures 3 (e,f). As expected the location of the amorphous area corresponds to the location of high stress field whereas the stress exists short ly beyond the amorphous precipitate.

Comparing Figures 3 (a,c,e) points out the different mechanisms of amorphization. Carbon-rich volumes as shown in Figure 3 (c) are amorphous (Figure 3 (a)) due to carbon induced amorphization. Despite decreasing carbon concentration amorphized volumes exceed the carbon maximas due to additional compressive stress. Even volumes with nearly zero carbon concentration are still amorphous until in the beginning of the crystalline surrounding still remaining stress is no longer sufficient enough for amorphization.

Figure 4 shows the carbon concentration in both, the amorphous and crystalline volumes for a simulation result similar to the 0-300 nm section of the cross sectional transmission electron microscopy image in Figure 1. Up to 160 nm all the carbon is located in crystalline volumes as amorphous volumes do not exist. With starting amorphization carbon concentration is reduced in the crystalline while increased in the amorphous phase. The heavy fluctuations result from the effect discussed in Figure 3 (c,d) and changing sizes of the amorphous precipitates in consecutive slices. Using linear regression would result in a graph  like the extrapolation of the linear part of the amorphous carbon concentration in both volumes.

Summary and conclusion

A simple model explaining the selforganization process of amorphous, lamellar precipitates during high-dose ion implantation is proposed. The simulation algorithm based on that model is described. Beside being able to reproduce experimentally observed formation of lamellar structures their evolution gets traceable by the simulation. The three different mechanisms contributing to amorphization are studied by variation of simulation parameters. Diffusion and resulting accumulation of carbon together with carbon induced and stress induced amorphization are responsible for the formation of ordered arrays of amorphous lamellae. Additionaly information that is not easily accessible by experiment, like the amorphous/crystalline state and carbon concentration in the target layers or the visualization of the stress field caused by amoprhous precipitates is now easily obtainable.

References

[1]	J.K.N. Lindner, M. Häberlen, M. Schmidt, W. Attenberger, B. Stritzker, Nucl. Instr. 	and Meth. B 186 (2002) 206-211

[2]	J.K.N. Lindner, Appl. Phys. A 77 (2003) 27-38

[3]	??

[4]	L. L. Horton, J. Bentley, L. Romana, A. Perez, C.J. McHargue, J.C. McCallum, 	Nucl. 	Intr. and Meth. B 65 (1992) 345.

[5]	W. Skorupa, V. Heera, Y. Pacaud, H. Weishart, in: F. Priolo, J.K.N. Lindner, A. 	Nylandsted Larsen, J.M. Poate (Eds.), New Trends in Ion Beam Processing of 	Materials, Europ. Mater. Res. Soc. Symp. Proc. 65, Part 1, Elsevier, Amsterdam, 1997, 	p. 114.

[6]	??

[7]	SRIM2000 Version of the TRIM program described by J.F. Ziegler, J.P. 	Biersack, U. 	Littmark in: The Stopping and Range of Ions in Matter, vol. 1, Pergamon Press, New 	York, 1985.

[8]	J.K.N. Lindner, W. Reiber, B. Stritzker, Mater. Sci. Forum Vols. 264-268 (1998) 	215-218.

die noch rein?

[X]	L.L. Snead, S.J. Zinkle, J.C. Hay, M.C. Osborne, Nucl. Instr. and Meth. B 141 	(1998) 123.

[X]	A.H. van Ommen, Nucl. Instr. and Meth. B 39 (1989) 194.

[X]	M. Ishimaru, R.M. Dickerson, K.E. Sickafus, Nucl. Instr. and Meth. B 166-167 (2000)	390.

Figure Captions

- XTEM image of a Si sample inplanted with 180 keV C+ ions at a dose of 4.3 x 1017 cm-2 and a substrate temperature of 150°C. Lamellar and spherical amorphous inclusions are marked by L and S.

- Several results of simulation runs with (a,b,c,d) different simulation parameter ps, (e,f) different diffusion rate dr and two runs with diffusion switched off (g) and on (h).

- Plane view display of amorphous (white) and crystalline (black) volumes in two consecutive layers m and m+1 (a,b) and corresponding carbon map (c,d) and stress map (e,f). Higher carbn concentrations and higher stresses are given by higher brightness in (c,d) and (e,f).

- Amoprhous crystalline view next to a rotated carbon implantation profile of the same simulation run. The implantation profiles show the amount of carbon in [at. %] of the amorphous, crystalline and both volumes.

1

2

3

4