Monte-Carlo-Simulation Study of the selforganization of nanometric amorphous precipitates in regular arrays during ion irradiation

F. Zirkelbach, M. Häberlen, J.K.N. Lindner, B. Stritzker

Universität Augsburg, Universitätsstrasse 1, D-86135 Augsburg, Germany.

# Abstract

PACS codes:

Keywords: 	Monte-Carlo Simulation, selforganization, precipitation, amorphization, nanostructures, ion irradiation

# Introduction

Owing to the statistical nature of collision processes, ion implantation into solids in a first place leads to disordered systems, such as depth profiles of different defects or distributions of precipitates with variable size. Ion implantation could be an elegant technique to create nanostructured surface regions, however, the statistics involed puts limits to those applications where existing fluctuations can be tolerated. These limits may be overcome by driving the system strongly by ion irradiation and simultaneously having mechanisms which counteract the irradiation effect. Under these circumstances selforganization can take place and allow for much more ordered systems to develope. Surface ripple formation during ion erosion is a prominent example for such an effect (sputtering is counteracted by surface diffusion), and implantation induced precipitate formation accompanied by ballistic precipitate destruction leading to narrow precipitate size distributions is an other.

In the present paper we explore a selforganization process which leads to regular arrays of amorphous spherical or lamellar nano-inclusions and which has been observed for a number of ion/target combinations, e.g. O+ or C+ implantation into Si, Ar+ into Al2O3 or Si+ into SiC. All these systems have in common that the amorphous phase has a largely reduced desity of host atoms compared to the crystalline host lattice. Therefore the amorphous inclusions exert compressive stress on the host matrix, leading to their selforganized spacial arrangement. In the present work we focus on high-dose carbon implantations into silicon.

# Mechanisms contributing to amorphization

If high-dose carbon implantations are performed at sufficiently high implantation temperatures to prevent complete surface amorphization and at the same time sufficiently low temperatures to prevent direct formation of crystalline 3C-SiC precipitates, it has been shown [] that the carbon supersaturation of the crystalline silicon (c-Si) matrix is reduzed by the formation of carbon rich amorphous precipitates (a-SiCx) with few nanometers in size. An example of amorphous nano-inclusions is presented in the cross-sectional transmission electron microscopy bright field images in Fig.1, showing amorphous lamellae and spheres in Si(100) implanted at 150 °C with 4.3 x 1017 cm-2 180 keV C+ ions. The precipitation of carbon in an amorphous a-SiCx phase helps the system to save the enormous interfacial energy which would be required if an interface was built up between crystalline 3C-SiC and c-Si with 20 % lattice mismatch. Pure amorphous silicon (a-Si) would not be stable against ion beam induced epitaxial recrystallization under the present implantation conditions, but small amounts of carbon are known to stabilize the a-Si phase []. Vice versa, the fact that the light C+ ions can amorphize c-Si at all at these elevated temperatures is attributed to the presence of carbon impurities, the effect termed “carbon induced amorphization” [].  Once small a-SiCx inclusions have been formed they may serve as diffusional sinks for excess carbon atoms in the c-Si phase (the room temperature solid solubility of C in c-Si beeing essentially zero). By this the a-SiCx phase can grow. Since the Si atomic density of stoichiometric amorphous SiC is 20-30% smaller than that of c-Si [], a reduced density is assumed also for relaxed substoichiometric a-SiCx. In the unrelaxed state the a-SiCx inclusions are assumed to exert compressive stress on their surrounding which decays by a r-2 law. This stress is partially compensated by arranging the a-SiCx spheres in regular arrays. Such local stress fields have been shown [] to enhance the local probability for further amorphization, as perfect crystall lattice restoration after an ion impact is less likely than in unstrained c-Si, leading to the formation of amorphous lamellae by connecting the amorphous spheres laterally. These lamellae develope preferentially parallel to the surface as strain relaxation perpendicular to the surface can be easily achieved. As a sum, there are mainly three mechanisms leading to amorphization, normal “ballistic” amorphization, carbon induced amorphization, and stress enhanced amorphization. It is assumed that ion beam induced amorphous to crystalline transitions can also occur, however,they are unlikely if the entire surrounding is already amorphized since then the necessary structural information is absent.

# Monte-Carlo Simulation